## Slide 1
Exploring Process Structure Linkages in Machined Chips
Patxi Fernandez-Zelaia
Ahmet Cecen
December 8, 2014
Material Informatics ME/MSE/CSE 8883

## Slide 2: Overview
Machining Introduction
Processing Effects on Microstructure
Problem Statement
Experimental
Image Processing
Data Analysis
Results
Conclusions

## Slide 3: Machining Introduction
Machining processes often follow primary shaping
Large imposed strains under high rate deformation
  Up to ~105 s-1, ε=~1-15
  Large temperature rise
“Large strain deformation and ultra-fine grained material by machining” Swaminathan et al. 2005

## Slide 4: Processing Effects on Microstructure
Thermo-mechanical loading induces microstructural evolution
  Grain refinement
  Dislocation density evolution
  Twinning
  …
“On the Metal Physical Considerations in the Machining of Metals” Ramalingam & Black 1972
“Large strain deformation and ultra-fine grained material by machining” Swaminathan et al. 2005

## Slide 5: Problem Statement
Manufacturing community has begun to study process-structure relationships in machining
Our goal is to explore process-structure linkages while quantifying structure gradients present in machined chips and
“A study of the interactive effects of strain, strain rate and temperature in severe plastic deformation of copper” Brown et al. 2009
250μm

## Slide 6: Problem Statement
Focus in this study is to first attempt to quantify gradients in the vertical direction (x-dir)
Analyze 7 unique processing conditions
Explore linkages in PCA space
250μm
x

## Slide 7: Experimental
Orthogonal cutting experiments performed varying:
  Feed (f)
  Cutting velocity (V)
Process conditions (f,V) affect thermomechanical processing and hence structure
CP-Ti (Gr 5) chips collected, etched and imaged using optical microscopy
5 images taken along the length of each chip
  Assuming all segments in a chip are representative of the imposed processing conditions
V
f
chip
workpiece

## Slide 8: Image Processing

## Slide 9: Image Processing

## Slide 10: Image Processing
20 Pixel Offset

## Slide 11: Image Processing
      Canny Edge Detection
      ( Gaussian Blur - > First Gradient - > Thresholding)

## Slide 12: Data Analysis
Chord Length Distribution

## Slide 13: Chord Length Distribution
Two distributions were considered
  (1) lacks sufficient sensitivity to quantify structure
  (2) weights larger chords and as such is more useful
P(X=x) probability that a chord is length x
P(X=x) probability that a pixel is found in a chord of length x
Chord length distribution displays expected trends. The reweighted distribution highlights longer length scales.

## Slide 14: Results
Top 50 Rows of Each Dataset
The dataset shows clear clustering across different Speeds, but does not separate well with Feed.

## Slide 15: Results
1
2
3
4

## Slide 16: Results
The dataset clusters well into distinct regions based on speed farther away from the machining surface, while showing very unstable clustering close to the surface.

## Slide 17: Machine Learning
Can we predict PC1 for any given speed given the three remaining speeds?
2.33 m/s
1.67 m/s

## Slide 18: Machine Learning
Can we predict PC1 for any given speed given the three remaining speeds?
1.00 m/s
0.33 m/s

## Slide 19: Results
Speed
A simple regression based learner provides stable estimates for interpolating and extrapolating vertical gradient from the machine surface.

## Slide 20: Etching Gradients
Acquisition Order

## Slide 21: Etching Gradients
All samples illustrated varying degrees of etch gradients
Sample 32 displayed greatest degree of etch gradient
Effects of etch gradient displayed in PCA space
Etch Gradient
Sample 32

## Slide 22: Future Work
More Reliable Imaging
  Different Polishing and Etching Techniques
  SEM
Nano-Indentation Data
  Alternative method for inferring local structure.
More refined discretization of speed/feed.
Incorporating cutting force measurements in to the learning process.
Accounting for the Etching Gradients

## Slide 23: Conclusions
Current techniques are fairly successful in classifying the structure towards the inner parts of the chips for the current dataset.
The current techniques cannot resolve information close to the machining surface as distinctly as the information farther away.
Uneven etching effects were found to be effectively captured by the principal components of chord length distribution.
Process path learning was demonstrated with variable accuracy on the given dataset. Substantial improvements were possible, but not explored, due to the current limitations and amount of data.

## Slide 24
Questions?